## Slide 1: Engineering and Medicine Coming Together to Cure Cancer Prof. Dipanjan Pan, PhD, FRSC, FAHA, FACC Associate Professor & Director of Professional Masters Program in Bioengineering University of Illinois at Urbana-Champaign; dipanjan@Illinois.edu; 217-244-2938

## Slide 2
Engineering and Medicine Integrated

## Slide 3
Next Generation Medicine
Tattoos that could block seizures
3D Printed Hearts
Muscle powered biobots walk on commands
3D printed heart socks to continuously monitor the heart’s electrical activity
Courtesy:
John Rogers,
Rashid Bashir
Wireless heart monitoring, improved IV lines, HIV detection

## Slide 4
Chemistry Basis, Medicine Centric & Eng Philosophy
Wet lab, In vitro, Ex vivo Studies, Clinical collaboration
Preclinical imaging
http://pan.bioengineering.illinois.edu
Clinical trials: 2
Start-ups: 3
Probes in the market: 2
Companion pet study: 1
Several patents
Technology licensing: 4
Large animal studies (Pig)

## Slide 5
Personalized, Degradable 3D Printed Trachea Stents
5
CT image of tracheal stenosis
CAD design and 3D Printing at UoI
3D Printed Stents
Traditional airway stents are made of silicone, metal, or hybrid materials--limited by their cost and complications such as migration and granulation tissue formation related to inaccurate stent size and shape. CT scanners extract 3D models of a patient’s trachea to guide the design of custom stent that are anatomically accurate with seamless surfaces that follow the contours of a patient’s airway

## Slide 6
Point of Care Diagnostics for Pulmonary Embolism
6
Current approach
Cardiac enzymes : markers found in the blood
Tested when Myocardial Infarction (MI) is suspected
Typically elevation of one of these markers are tested (heart muscle damage)
New approach:
Simultaneous detection of 4 biomarkers & B-type natriuretic peptide (BNP)
Better prediction
Accurate analysis
Better management

## Slide 7
Symptoms
Clinical Symptoms
Screening
Early
Diagnosis
Preventive
Treatment
Current symptomatic medicine
leads to chronic disease
Functional and quantitative imaging localizing the disease
Follow response to therapy
Minimally invasive treatment
management tailored to the patient
From Symptomatic to Pre-emptive Medicine
Disease progression
Time
Preemptive medicine

## Slide 8
Translational Nanomedicine
Whole body Organ Tumor Blood Clot Angiogenesis Cells
Multidisciplinary approach to early detection
Angew Chem 2009; 2010
JACS 2008; 2009; 2010; 2011; 2012; 2017
ACS Nano 2011; 2012; 2015

## Slide 9
Molecular Imaging
LV
SLN
Thrombus
Angiogenesis
Imaging
Probes (Exploratory)
Sentinel Lymph Node
Drug Release
Intra-cellular
ACS Nano. 2012;6(4):3364-70.
Small. 2015;11(36):4691-703.
Sci Rep. 2016; 6:29299.
Collaborator: Rohit Bhargava
Collaborator: Rohit Bhargava
Nanoscale, 2016, 8, 2826-2831
Small. 2016
Nanomedicine. 2015; 11(3):569-78.
JACS. 2012;134(25):10377-80.
Collaborator: Philips, Lanza, Wickline
Molecular Imaging
Sci Rep. 2015; 5:14986.
Theranostics. 2013;3(9):677.
ACS Nano. 2012; 6(2):1260.
Angew Chem 2010;49(50):9635.
Collaborator: Lihong Wang
Atherosclerosis
JACS. 2011;133(24):9168-71.
Collaborator: Philips, Lanza, Wickline

## Slide 10
Therapeutics
Combinatorial therapy
Transcription factors
Oncogenes
Stem-like Cells
Trans arterial chemo-embolization (TACE) for liver cancer
Metabolic therapy
pH therapy
Nuclear Receptor
Locally delivered US ablation
Thrombus
Target defects in cancer cells
Carry other drugs to a tumor
Apoptosis
Immuno therapy
Prevent/Block Cell Growth
Therapy
Signaling pathways inhibition by stem cell targeting
ACS Nano 2015
Sci Rep 2016
Sci Rep 2015
Mol Can Ther 2017
Sci Rep 2014
ACS Applied Mat Int, 2017
Sci Rep 2016
Biomaterials 2010

## Slide 11
How Early We are Able to Detect?

## Slide 12
720 nm
720 nm
720 nm
Is it Possible to Detect Neo-angiogenesis?
Red arrows denote small neovascular sprouts arising from immature angiogenic vessels with only nascent blood flow.
Early detection of immature, nascent angiogenic
vessels with Photo-acoustics Imaging and GNB!
FASEB J, 25, 875-882
MATRIGEL MOUSE MODEL
14 days
80-150nm
Au
Integrin avb3-Targeted
Gold NanoBeacons (GNB)
avb3-GNB
The specificity of αvβ3-integrin-NP was demonstrated by inhibiting αvβ3-transfected K293 cell binding to vitronectin. Effective affinity = 50 pM (per particle).
300 copies / Gold Nanoparticle

## Slide 13
Early Neovascular Response to Acute Lung Ischemia using Simultaneous 19F/1H MR Molecular Imaging

## Slide 14
Whole body 19F/1H images of Rat Thorax & Abdomen
A. Coronal plane of rat showing accumulation in left lung near the pulmonary artery ligation site (adjacent to heart) and diffuse accumulation in the lung parenchyma. Minimal signal was detected in the right lung.
B. Sagittal view. C. Transverse view at the level of the heart showing bound nanoparticles in the left but not in the right lung.
D. Coronal plane of rat following NT-nanoparticles showing no visual accumulation in the injured left lung adjacent to heart, but with significant RES clearance of particles into the liver and spleen.
αvβ3-targeted nanoparticles can be used to directly measure neovascularity in a rat left pulmonary artery ligation (LPAL) model employed to create pulmonary ischemia and induce angiogenesis.
Angiogenesis 2014

## Slide 15
Whole body 19F/1H images of Rat Thorax & Abdomen
Comparison of left and right lung 19F signal normalized to background noise within injured rats receiving αvβ3-targeted perfluorocarbon nanoparticles. Left lung 19F signal is significantly greater (p=0.009) than right lung contrast.
Comparison of left-right lung signal in day 3 LPAL rats, and sham-operated rats, administered nontargeted, αvβ3-targeted, or competitive-inhibited αvβ3-targeted nanoparticles after two hours.
Angiogenesis 2014

## Slide 16
TACE for Lung Cancer

## Slide 17
Transarterial Chemo Embolization in Lung Cancer
A
Fluoroscopy (X-ray)
Volume rendered overlay of selective signal of contrast (yellow) in its spatial relation to surrounding bone structures (rabbit)
B
K-edge Imaging (Color CT)
Radio-opaque Thermo-responsive Polymeric Agent for Occlusion
Patients with advanced or recurrent lung cancer have lesions invading the mediastinum with serious symptoms. Selective arterial infusion of antineoplastic agents will concentrate the drugs in the target lesion and reduces systemic exposure

## Slide 18
Radiofrequency Ablation (RFA) and Repurposed Drug for Non-Small Cell Lung Cancer

## Slide 19
Retinoid X Receptor (RXR)
NANO
MEDICINE
Drug Repurposing
New Drug
Discovery
PRODRUG STRATEGY
+ MAGIC BULLET
Orphan Nuclear Receptor
Cancer

## Slide 20
RFA limitations and Advantage of Trimodal Therapy
Therablob
Ablation Zone
Thermal Zone
RFA misses micro-metastases outside ablation zone
Therablob + RFA:
Trimodal therapy: hyperthermia+ sonoporation + chemo
Image-guided catheter-based delivery of prodrug-nanobubbles
Patented self-assembled prodrug nanobubble therapy
Drug concentrates in the “Thermal Zone”
Ablation releases selective drug expanding treatment area and destroying micro-metastases
RFA Electrode

## Slide 21
Nanobubbles Derived from Activatable Prodrug
Treatment for Cancer
This treatment might be an option for some people some small lung tumors that are near the outer edge of the lungs, especially if they can’t tolerate surgery.
Derived from repurposed FDA approved agents
Remarkable specificity
ACS Nano 2015
(Bexarotene)

## Slide 22
US Triggered Delivery
A
New class of nanobubble derived from SN2 RXR prodrug
Fluoroscopy (X-ray)
Rodent
Pig

## Slide 23
Ultrasound Induced Bursting
Shock wave
0 ns 60 ns 62 ns 63 ns 65 ns
(Collaborator: K. Schulten, E. Tajkhorshid)

## Slide 24
Membrane Funnel Formation, No Pore
Jet flow membrane “punching”
Prodrug spontaneous insertion
Prodrug post-ultrasound delivery relies on spontaneous membrane insertion!

## Slide 25
Cell Internalization Mechanism
Inhibitor pre-incubation
study.
(B-D) Cell TEM of Prodrug-NP after 30 min of incubation showing position of membrane fusion as mode of cellular entry.
Cell with rhodamine alone (E, F) and Rh-Pro-NPs (G, H). E&G: DAPI stained cellular nucleus; F &H: Rh distributed in intracellular space (4h).

## Slide 26
Flexible Catheter Based US Ablation System
Catheter-Based Ultrasound (CBUS) Applicators for Percutaneous Conformal Hyperthermia and Thermal ablation to Targets in Soft Tissue

## Slide 27
Flexible Catheter Based US Ablation System
Collaborator: Acoustic Medsystem
(a)
(b)
(c)
Injecting Therablob
(b) US B-mode image of the tissue (yellow arrow indicate the release of the TheraBlob into the tissue as can be visualized in the B-mode image,
(c) applicator

## Slide 28
Remarkable Efficacy in Transgenic Pig Model
Histopathology images of (a) normal tissue,
(c) treated with US only, and (g, h, i) US + TheraBlob.

## Slide 29
New Chemotherapeutics

## Slide 30
From RXR Discovery to Controlled Delivery (Preclinical)
Progression of computational, chemical and biological experiments
Hetero-dimerization capacity with RAR, LXR, PPAR, etc.
Transcriptional activation to induce apoptosis, cellular differentiation
Current RAR-drugs in clinical trials: 11; RXR-drugs in clinical trials: 2
Rexinoids (RXR selective ligands): activities on multiple pathways.
High selectivity (from RAR) is the key factor for the new design of RXR ligands with less toxicity
Collaborator: Larry Schook (Oncopig)

## Slide 31
In vivo Tumor Regression Studies in Mouse Xenograft
Tumor volume regression post treatment with RXR and Nano-RXR whereas nanoparticles alone (RCM) or untreated animals were used as controls.
Protein expression in tissues collected from treated and untreated group of animals.
1: Buffer; 2: RCM; 3: RXR and 4: Nano-RXR from (i) tumor tissue and (ii) tissue from liver.
Post effects on protein expression

## Slide 32
In vivo Tumor Regression Studies in Transgenic Pig
a) Timeline of in vivo experiment in onco-pig model. Tumor appearance on (b) day 1 of buffer injection.
(c) Tumor volume regression post treatment with RXR and Nano-RXR whereas animals treated with buffer were used as controls.

## Slide 33
Post Effects on Protein Expression
Protein expression in tissues collected from treated and untreated group of animals.
1: Buffer; 2: RCM; 3: RXR and 4: Nano-RXR as obtained from (i) tumor tissue and (ii) tissue collected from liver.
US imaging to follow tumor growth
Nano-RXR
Buffer
Day 1
Day 13

## Slide 34
Drug Metabolism Genes in Liver and Tumor
RXR and Nano-RXR induced transcriptional alteration of genes involved in phase-I and phase-II drug metabolism, phase-III transport and nuclear receptors in liver and tumor measured by qPCR.
Liver: CYP2C33, CYP2E1 and PXR were downregulated, SULTA1, FXR and PPARγ were unchanged and the rest of the genes were upregulated.
Tumor: FXR was downregulated, CYP1A2 was unchanged and all the other genes were upregulated by treatment.

## Slide 35
Acknowledgement
Peter J Stang, PhD (OSU)
Allan Doctor, MD (WUSM)
Sam Wickline, MD (WU/USF)
Greg Lanza, MD, PhD (WUSM)
Babak Razani, MD (WUSM)
Pritesh Patel, MD (UIC)
Damiano Rondelli, MD (UIC)
Rohit Bhargava, PhD (UIUC)
Larry Schook, PhD (UIUC)
Klaus Schulten, PhD (UIUC)
Blair Rowitz, MD (Carle)
Leanne Labriola, DO (Carle)
Rashid Bashir (UIUC)
Joseph Irudayaraj (UIUC)
Michael Oelze (UIUC)
Pan Lab @ Illinois
Funding
Start-ups
Collaborators
http://pan.bioengineering.Illinois.edu

## Slide 36
http://pan.bioengineering.Illinois.edu
Thank You
Look forward to answering questions and collaboration